## Slide 1: Development of Spiropyran Immobilization and Characterization Protocols for Reversible Photo-Patterning of SiO2 Surfaces
Bokun Zhou, Ph.D. Candidate in Materials Science
Remcho Research Group
Oregon State University
Presented on: November 28, 2023
Presentation Number: EL06.05.07

## Slide 2: Properties of Spiropyran
Spiropyran (SP)
hydrophobic, colorless
closed form
Merocyanine (MC)
hydrophilic, purple
open form
Background
[1] R. Klajn, “Spiropyran-based dynamic materials,” Chem. Soc. Rev., vol. 43, no. 1, pp. 148–184, 2014, doi: 10.1039/c3cs60181a.
Benzopyran
Indole
MC form is fluorescent at red 630nm[1]
Sensitive to various stimuli [1]
Light
Temperature
pH
Solvent polarity
Metal ions
Redox potential
Mechanical stress
Chemical structure of a common spiropyran
Photochromism
  Reversible conversion
  Triggered by lights
UV-VIS spectra of SP, MC and protonated MC[1]
MC Absorption Peak

## Slide 3: Spiropyran Applications with SiO2
Background
Silicon wafer
Change of contact angle[1]
Silica capillary
Capillary-integrated optical sensor[2]
Silica, mesoporous
Size changes (pH); drug delivery [3]
Silica, mesoporous
Ring-opening (pH); drug release [4]
Silica, mesoporous
Pore size affect kinetics [5]
Silica, dendritic fibrous
Photo-induced adsorption[6]
Silica, nanoparticle
Adsorption of fluoride contamination [7]
Silica, microbeads
Metal ion extraction [8]
Silicon wafer
Change of contact angle[1]
Silica capillary
Capillary-integrated optical sensor[2]
Silica, mesoporous
Size changes (pH); drug delivery [3]
Silica, mesoporous
Ring-opening (pH); drug release [4]
Silica, mesoporous
Pore size affect kinetics [5]
Silica, dendritic fibrous
Photo-induced adsorption[6]
Silica, nanoparticle
Adsorption of fluoride contamination [7]
Silica, microbeads
Metal ion extraction [8]
Substrates and Applications

## Slide 4: Spiropyran Applications with SiO2
Background
Silicon wafer
Change of contact angle[1]
Silica capillary
Capillary-integrated optical sensor[2]
Silica, mesoporous
Size changes (pH); drug delivery [3]
Silica, mesoporous
Ring-opening (pH); drug release [4]
Silica, mesoporous
Pore size affect kinetics [5]
Silica, dendritic fibrous
Photo-induced adsorption[6]
Silica, nanoparticle
Adsorption of fluoride contamination [7]
Silica, microbeads
Metal ion extraction [8]
Porous Substrate
Porous Substrate
Porous Substrate
Porous Substrate
Porous Substrate
Porous Substrate
Aim of this work
Robust immobilization, optimized
Quick and effective characterization
Non-covalent bonded
Non-covalent bonded
Silane coupling
w.
SP polymer
Silane coupling
w.
customized SP
Silane coupling
w.
customized SP
Silane coupling
w.
carboxylic SP
Thermal hydrosilylation
Silane coupling
w.
customized SP
Substrate Types and Bonding Methods

## Slide 5: Technical Approach (this work)
Method
-OH groups
-NH2 terminated crosslinker
Merocyanine (MC)
SiO2
Si substrate
Activation
SiO2
Si substrate
Amination
SiO2
Si substrate
Functionalization
SiO2
Si substrate
Bare substrate

## Slide 6: Immobilization: effective activation and amination
Selected Activation Methods
Oxygen plasma treatment
Acid treatment (1M HCl)
Piranha solution: (H2SO4 + H2O2)
Results
 | C 1s | O 1s | Si 2p | Contact Angle
Untreated SiO2 Surface | 2.8% | 67.1% | 30.1% | 60°– 70°
Activated with O2 plasma | 3.8% | 67.5% | 28.8% | 10°– 15°
Activated with HCl | 2.8% | 67.6% | 29.6% | 10°– 15°
Activated with H2SO4 | 2.7% | 67.6% | 29.7% | 10°– 15°
Surface Atomic Concentration by XPS and Contact Angle
Activation Step
Amination Process Condition | C 1s | O 1s | Si 2p | N 1s | % organosilicon* | N : % organosilicon
2% APTES 5min@RT | 22.4% | 50.7% | 24.1% | 2.8% | 2.7% | 1.0
2% APTES 10min@RT | 40% | 36.9% | 18.0% | 5.1% | 4.7% | 1.1
Surface Atomic Concentration Table by XPS
Amination Step
C9H23NO3Si
*: from the immobilized APTES
C9H23NO3Si

## Slide 7: Immobilization: thin layer of APTES amination
Results
To reduce self-reaction
  Freshly prepared APTES solution
  2% APTES at room temperature for 5min  0.5 – 0.7 nm
From XPS results, N:% organosilicon is approximately 1:1.
Together, the results verifies a successful thin layer amination.
APTES
Thickness
SiO2
Si substrate
Ellipsometry Model
Incident light
Reflected light
Thin layer, ideally mono-layer
Incubation with APTES
Reaction Time
Reaction Temperature
APTES Concentration

## Slide 8: Immobilization: functionalized surface with fluorescence
Results
1-(3-Dimethylaminopropyl)-3-ethylcarbodiimide hydrochloride (EDC)
SiO2
Si substrate
Ex.
550nm
Em.
640nm
No emission with SP form
MC-immobilized SiO2 sample
20x, 1s
MC
SP
MC-immobilized glass microfiber sample
20x, 10ms
20x, 10ms
MC
SP
SiO2
Si substrate
SiO2
Extracting RGB value from fluorescence images, taken at setting of 20x, 20ms
Incubation with SP-COOH and EDC
EDC-mediated coupling of carboxylic acids and amines

## Slide 9: Summary and Future Work
Surface density of functional groups
  -OH is limited by surface type
    On average, there are 4.9 #/nm2 OH groups on amorphous silica.[1]
Sensitivity of fluorescence detection
  Measurement setup
  MC-SP conversation
  Low quantum yield of MC fluorescence
Immobilization Protocol
  Effective activation
  Thin layer amination
  Fluorescence functionalization
Discussion
[1] L. T. Zhuravlev, “Concentration of hydroxyl groups on the surface of amorphous silicas,” Langmuir, vol. 3, no. 3, pp. 316–318, May 1987, doi: 10.1021/la00075a004.
2-Naphthoyl chloride
Ex/Em = 265nm/380nm
Proposed Scheme to Further Modify Surfaces
(lock in MC form & enhance fluorescence)
Characterization Protocol: XPS, contact angle, ellipsometry, fluorescence
  Change in surface chemistry / surface energy
  Controlled thickness growth
  Reversible photo-patterning and fluorescence

## Slide 10: References
Review Paper
[1] R. Klajn, “Spiropyran-based dynamic materials,” Chem. Soc. Rev., vol. 43, no. 1, pp. 148–184, 2014, doi: 10.1039/c3cs60181a.
Spiropyran Application with SiO2 Surface
[1] D. Dattilo, L. Armelao, G. Fois, G. Mistura, and M. Maggini, “Wetting Properties of Flat and Porous Silicon Surfaces Coated with a Spiropyran,” p. 6, 2007, doi: 10.1021/la7024878.
[2] L. Florea, A. Hennart, D. Diamond, and F. Benito-Lopez, “Synthesis and characterisation of spiropyran-polymer brushes in micro-capillaries: Towards an integrated optical sensor for continuous flow analysis,” Sensors and Actuators B: Chemical, vol. 175, pp. 92–99, Dec. 2012, doi: 10.1016/j.snb.2011.12.055.
[3] Y. He et al., “pH-Responsive size-shrinkable mesoporous silica-based nanocarriers for improving tumor penetration and therapeutic efficacy,” Nanoscale, vol. 14, no. 4, pp. 1271–1284, 2022, doi: 10.1039/D1NR07513F.
[4] R. Han, S. Wu, K. Tang, and Y. Hou, “Facilitating drug release in mesoporous silica coated upconversion nanoparticles by photoacid assistance upon near-infrared irradiation,” Advanced Powder Technology, vol. 31, no. 9, pp. 3860–3866, Sep. 2020, doi: 10.1016/j.apt.2020.07.025.
[5] T. Yamaguchi, N. N. Leelaphattharaphan, H. Shin, and M. Ogawa, “Acceleration of photochromism and negative photochromism by the interactions with mesoporous silicas,” Photochem Photobiol Sci, vol. 18, no. 7, pp. 1742–1749, Jul. 2019, doi: 10.1039/c9pp00081j.
[6] T. Yamaguchi, A. Maity, V. Polshettiwar, and M. Ogawa, “Photochromism of a Spiropyran in the Presence of a Dendritic Fibrous Nanosilica; Simultaneous Photochemical Reaction and Adsorption,” J. Phys. Chem. A, vol. 121, no. 42, pp. 8080–8085, Oct. 2017, doi: 10.1021/acs.jpca.7b08466.
[7] X. Guan, M. He, J. Chang, Z. Wang, Z. Chen, and H. Fan, “Photo-controllability of fluoride remediation by spiropyran-functionalized mesoporous silica powder,” Journal of Environmental Chemical Engineering, vol. 9, no. 1, p. 104655, Feb. 2021, doi: 10.1016/j.jece.2020.104655.
[8] S. Scarmagnani et al., “Photoreversible ion-binding using spiropyran modified silica microbeads,” IJNM, vol. 5, no. 1/2, p. 38, 2010, doi: 10.1504/ijnm.2010.029921.
Limitation on –OH Surface Density
[1] L. T. Zhuravlev, “Concentration of hydroxyl groups on the surface of amorphous silicas,” Langmuir, vol. 3, no. 3, pp. 316–318, May 1987, doi: 10.1021/la00075a004.
Reference

## Slide 14
MC-immobilized PMMA sample
20x, 20ms
MC
SP
PMMA
Chart: Contrast of Red Value between MC and SP
| 1,8-diaminooctane on PMMA | 1,4-diaminobutane on PMMA | Mix of 1,4- and 1,8-diamines on PMMA | APTES on PMMA | APTES on SiO2
Red Signal | 25 | 51 | 37 | 23 | 12.1

## Slide 15: Process and Characterization Flowchart: SiO2 Surface
sample pretreat
start
piranha activation
Acetone/IPA/DIW rinse, Dry with N2
Oxygen plasma clean
Bake at 115°C for 5min
Immerse in piranha solution (H2SO4:H2O2=3:1) for 30min
Immerse and rinse with DIW, dry with nitrogen
Immerse sample into SP-COOH solution, incubate + shake for 16 hrs.
Rinse with ethanol and DIW, Dry with N2
SiO2 substrate
1”x1” coupon
Substrate pretreat
Activation
rinse
Rinse and sonicate with ethanol, Bake at 115°C for 5min
Contact Angle
Check change in thickness by ellipsometry
UV irradiation
Use UV light to gate the spiropyran in MC form
Modification
2-NC
modification
sonication and baking
EDC+SP-COOH
SP-COOH
immobilization
Prepare SP-COOH 2 mg/ml + EDC 1.5 mg/ml in 75% ethanol, incubate + shake for 30min
Prepare stock solution 2% APTES in ethanol
Amination
Functionalization
Fluorescence Microscopy
Check fluorescence from MC or other fluorescence tags
Characterization
Ellipsometry
Check change in contact angle
APTES
amination
APTES Solution
Immerse coupon into 2% APTES solution at room temperature for 5min
Immerse in 2-NC + TEA solution for 4 hrs.
Rinse with ethanol and DIW, dry with N2

## Slide 16: Immobilization Mechanism: Carbodiimide Crosslinker
1-(3-Dimethylaminopropyl)-3-ethylcarbodiimide hydrochloride
1,8-diaminooctane
Mechanism of EDC-mediated coupling of carboxylic acids and amines
EDC
Diamine
1, 8-diaminooctane
1, 4-diaminobutane
Carboxylic acid
carboxyl groups (-COOH) on activated SU-8 surface
carboxylic spiropyran (SP-COOH)